## Slide 1
JAIST — Taniike Lab
Integrating OCM Literature Data into Lab-Scale ML Models
A Walkthrough of Five Transfer-Learning Approaches
Partha Nupam Nagar
June 2026
OCM Dataset Integration | Slide 1 / 12

## Slide 2
The Problem — Two Datasets, Three Systematic Differences
OCM Dataset Integration | Slide 2 / 12
Our Lab Data
Samples
89,074
Year
2025
Preparation
Impregnation only
Mean Y(C2)
5.25%
Conditions
Fixed, one lab
Published Literature (≤2019)
Samples
3,852
Year
1982 – 2019
Preparation
15+ methods
Mean Y(C2)
8.67%
Conditions
40 years of diverse labs
Can we use literature to improve our model — without hurting it?
1. Label shift
Literature mean is 3.42 pp higher (t = −32.2, p < 10⁻²⁰⁰) — a systematic offset from publication bias and optimised conditions.
2. Covariate shift
78.5% of literature samples describe chemistry our lab has never tested.
3. Publication bias
Literature is skewed, not just shifted — failed experiments are rarely reported, over-weighting high yields.
Why ML? The catalyst search space (65 elements × varying loadings × temperature) is too large to screen physically. A surrogate model guides experiments toward high-yield compositions.

## Slide 3
Visualising the Gap — Label Shift, Covariate Shift, Chemistry
OCM Dataset Integration | Slide 3 / 12
Top: label & covariate shift
• Red band = 3.42 pp mean gap
• Orange tail = publication-bias skew
• PCA: orange spreads outside blue cluster
Bottom: which elements differ?
• Different active phases / promoters
• Concrete chemistry, not abstract
• Justifies selective filtering
These three figures jointly forecast that naive concatenation will harm the model — confirmed on slide 5.

## Slide 4
How We Measure Success — Asymmetric 5-Fold CV
OCM Dataset Integration | Slide 4 / 12
The validation rule
• Our 89,074 samples split into 5 folds
• Training fold = 4/5 of our data + any literature
• Validation fold = 1/5 of our data only
• Literature never appears in validation
Why asymmetric?
• The question: how well does the model predict OUR experiments?
• Mixing literature into validation would dilute the answer
• Same CV harness used for every method — only training data changes
Metric: RMSE
in units of percentage points of C₂ yield. An RMSE of 2.1 means typical error ≈ 2 pp.
5-fold split (our data, n=89,074)
fold 1 train
fold 2 train
fold 3 VAL
fold 4 train
fold 5 train
+ literature (training only, never validation)
Repeat 5 times, rotating which fold is the validation set. Report mean RMSE ± std.

## Slide 5
Baseline + Why Naive Merging Fails
OCM Dataset Integration | Slide 5 / 12
Step 1 — establish baseline
Method
CV RMSE
Baseline (our data only)
2.133
Number every method must beat.
Step 2 — try the obvious
Method
CV RMSE
Baseline
2.133
Naive merge (3,852 lit rows)
2.248
+5.4% worse than baseline.
Why did it fail?
Model sees two catalysts with nearly identical composition:
• One labelled 5.2% (our lab)
• One labelled 8.7% (literature)
No feature explains the gap — flow rate, gas ratio, etc. are absent. The model hedges and predicts both badly.
The 3.42 pp offset is a SYSTEMATIC signal the model cannot account for — and incorrectly tries to fit. Mixing the two datasets can perform WORSE than using ours alone. ⇒ We need to be much more selective.

## Slide 6
DRST — Filtering by Chemical Similarity
OCM Dataset Integration | Slide 6 / 12
Histogram of P(ours | x) for every literature sample. Dashed lines = candidate thresholds.
How it works
• Train logistic classifier (finds element-space boundary): ours=1, lit=0
• Score each lit sample: P(ours | x)
• Keep samples scoring ≥ τ
The classifier's confidence P(ours | x) is a similarity score: high = looks like our chemistry, low = foreign. We keep only literature scoring above τ.
Threshold sweep
τ
kept
RMSE
τ = 0.10
1168 kept
2.068
τ = 0.20
987 kept
2.034
τ = 0.30
782 kept
2.019
τ = 0.40
543 kept
2.045
Unsolved: hard cutoff is arbitrary — a sample at 0.29 is fully discarded; 0.31 gets full weight.

## Slide 7
KMM — Soft Weights Instead of a Hard Filter
OCM Dataset Integration | Slide 7 / 12
How it works
• Each lit sample gets weight wᵢ ∈ [0, 10]
• RBF kernel similarity: K(x,x′) = exp(−‖x−x′‖²/2σ²)
• Solve QP: ½ wᵀK_ss w − κᵀw
• σ via median heuristic (parameter-free)
KMM picks weights so the weighted literature cloud matches our data cloud. Samples inside our chemistry earn weight; those outside fade to zero.
Result
KMM CV RMSE
2.035
Δ vs baseline
−4.6%
Near-zero weights
78.5%
Agreement w/ DRST
r = 0.79
Reassuring: two unrelated methods flag the same 78.5% of samples ⇒ real signal, not artifact. Still unsolved: literature labels remain in training, so the 3.42 pp offset still bleeds in.

## Slide 8
Prior Feature Transfer — The Winning Pipeline
OCM Dataset Integration | Slide 8 / 12
STAGE 1 — Pre-train on Literature Chemistry
STAGE 2 — Fine-tune on Our Labels Only
Literature
3,852 samples (DRST filtered)
Stage 1
XGBoost pre-train
lit_prior
prediction (68th feature)
Our Lab Data
89,074 samples
Append
68th feature
Stage 2
LightGBM our labels only
Prediction
Y(C₂) %
Key property — literature enters as a feature, not a label
Stage 2 NEVER sees literature labels. The 3.42 pp offset affects the VALUE of the 68th feature — which Stage 2 can calibrate: "when the expert says 8, my lab gets ~4.5". It does NOT corrupt the training loss, which it could not fix. A corrupted label can't be un-corrupted; a feature value is just another thing to learn around. Stage 1 uses XGBoost (conservative on 782 rows); Stage 2 uses LightGBM (fast on 89,074 rows).

## Slide 9
Results — All Five Methods at a Glance
OCM Dataset Integration | Slide 9 / 12
Cross-validation (our data)
Method
RMSE
Δ
Naive merge
2.248
+5.4%
Baseline
2.133
—
KMM weighted
2.035
−4.6%
DRST (τ=0.30)
2.019
−5.3%
Prior FT ★
1.907
−10.6%
OOD robustness (unseen lit)
Method
OOD RMSE
Baseline
6.53
Prior FT ★
3.60 (−45%)
OOD: 2,139 non-Impregnation lit samples, unseen.

## Slide 10
SHAP — Did the Model Learn Real Chemistry?
OCM Dataset Integration | Slide 10 / 12
Top findings (3,000 sample subsample)
• #1: lit_prior_prediction — transfer is genuinely used
• Temperature — strong positive, T↑ → C₂↑
• Ba, Mn, La, Ce — known OCM active phases / promoters
• Li, K — mixed / suppressive effect
Residual pattern (ceiling effect)
Y(C₂) range
RMSE
0 – 6%
1.43 – 1.48
6 – 10%
1.95
10 – 15%
2.58
> 15%
4.70 (−4.2 pp bias)
Root cause: GHSV, CH₄/O₂ ratio, pressure absent from dataset — a data limit, not a model failure.

## Slide 11
Critical Analysis & Next Steps
OCM Dataset Integration | Slide 11 / 12
Honest critique of each method
Method
Main limitation
Naive merge
Negative control only — harms the model
DRST
Hard cliff; discards ~80% of lit; τ tuned on the reported CV
KMM
Slow n×n kernel; σ-sensitive; still uses labels; ties DRST
Prior FT
Best — but Stage-1 on 782 rows → high variance; two models
Cross-cutting limits
• Scored on our-data CV only; OOD checked for Prior FT alone
• Point predictions — no uncertainty for picking experiments
• Y>15% ceiling is DATA-bound, not model-bound
What's next (priority-ordered)
1.
Add GHSV, CH₄:O₂, pressure — fixes the ceiling and likely the label shift
Highest impact
2.
Bag the Stage-1 expert to cut its variance
3.
Add uncertainty (quantile / conformal) for experiment selection
4.
Stack DRST + KMM into the Prior FT pipeline
5.
Neural domain adaptation (DANN / CORAL) once features are richer
6.
Close the active-learning loop: propose → measure → retrain

## Slide 12
Summary
OCM Dataset Integration | Slide 12 / 12
What we asked
Can published OCM literature improve a lab-data model without harming it?
What we learned
• Naive merging HARMS accuracy (+5.4% RMSE) — the systematic offset corrupts training.
• Selective filtering (DRST / KMM) recovers about 5% improvement — independent methods agree (r=0.79).
• Using literature as a PRIOR FEATURE (not a label) gives the biggest gain: −10.6% CV, −45% OOD.
• SHAP confirms the model uses real OCM chemistry: temperature, Ba, Mn, La, Ce, and the literature prior drive predictions.
Next step that matters most
Add GHSV and CH₄:O₂ to the feature set — the high-yield ceiling is data-bound, not model-bound.